po box 188 Boone, NC 28607

tele 828-266-1599

www.bdwgconcretestudio.com

Countertops –Sinks- Shower and Bath - Acid stained Floors- Furniture

Residential/Commercial - Professional Construction Services

Guidelines for Concrete Floors

General Guidelines

- If slab is to be poured over a wood sub-floor use 15lb. roofing paper as a vapor barrier between wood                               and concrete.

- The thickness of the slab can be as thin as 2” when sub-floor is engineered for added support.

- 2” concrete weighs approx. 25lbs. Per sq. ft.

- Concrete should be 4,000 psi or greater.

- Small aggregate or “chat-mix” is desired.

- Add fiber and other reinforcement where required.

- Plan for control joints if necessary.

- Follow good concrete practices for conditions.

- Hard-trowel finish.

# Specific Guidelines for Concrete that is to be Stained

## Curing

- Freshly poured slab should be covered completely with black plastic within the first 12-24 hrs. after slab is poured.

- Tape all joints and seal edges to completely encase the freshly poured concrete.

- NEVER use any liquid curing compounds or sealer on a slab that is to be stained.

- DO NOT use tape to adhere plastic to concrete.

- Concrete should be covered for a minimum of 7 days.  If possible slab should be covered for 30 days.

## During Construction

- Concrete slab should be protected from all contaminants i.e. sheetrock mud, glue, stains, paint overspray or drips, mud, grease and oils.

- Keep slab covered with plastic sheeting, do not place blue-board or plywood directly on concrete.

- Decorative stain-work should take place after construction towards the very end of the project.

- It is preferred to run all base board after slab is stained and sealed.

- The scoring, staining and sealing process is 3-5 days.

### Care and Cleaning

- Sweep, vacuum, or mop regularly.

- Do not use abrasive cleaners on sealed concrete.

- Finish can be maintained by applying an acrylic safe floor-finish, such as Mop & Glow periodically as needed.

*** Following these simple guidelines will help keep costs down and ensure that your slab can be successfully stained to create a beautiful, low maintenance flooring surface that you and your clients will be pleased with.